## Slide 1: NNUF Access Fund #186
Fast non-destructive characterisation of nuclear fuel pellets via hyperspectral imaging
A.J. Parker1, R.D. Dunphy2, P. Murray2, R. Wilbraham1, and J. Zabalza*2
1Lancaster University, Lancaster, LA1 4BE
2University of Strathclyde, Glasgow, G1 1XQ
*Proposal Submitted by

## Slide 2: Hyperspectral Imaging Overview
Intensity
Spectrum
λ
x
y
Ultraviolet
Infrared
Via University of Strathclyde's Hyperspectral Imaging Centre
J. Zabalza, et al, IEEE Sensors Journal, Vol 23, No. 21 2023
VNIR
400-1000 nm
Example – identifying corrosion on nuclear packages
SWIR
1000-2500 nm
HSI for NNUF

## Slide 3: Background I
EPSRC funded project, Autonomous Inspection for Responsive and Sustainable Nuclear Fuel Manufacture.
Preliminary measurements of UO2 SIMFuel pellet slices* in UTGARD inventory
SWIR spectra of SIMFuel by type
Photo of SIMFuel pellet slices
SIMFuel source no. and type
* Z. Hiezl, D. I. Hambley, C. Padovani, and W. E. Lee, “Processing and microstructural characterisation of a UO2-based ceramic for disposal studies on spent AGR fuel,” Journal of Nuclear Materials, vol. 456, pp. 74–84, 2015, doi: 10.1016/j.jnucmat.2014.09.002.

## Slide 4: Background II
Continuation of testing on x8 pure UO2 AGR design and NNL Preston
Observed same SWIR response for pure UO2 as initial undoped SIMFuel
SWIR spectra of pure UO2 AGR pellets
Photo of AGR fuel pellets and SWIR camera setup

## Slide 5: NNUF Access Fund & Industrial Relevance
Seeing a clear distinction being fresh fuel and spent fuel
Change in response likely due to presence of fission products
We wanted to know which fission products (if any) was causing this..
SWIR spectra of pure UO2 AGR pellets
SWIR spectra of SIMFuel by type

## Slide 6: Pellet Preparation
UTGARD and ADRIANNA laboratories at Lancaster
Spark plasma sintering to produce UO2 pellets – Split SIMFuel
Raman and SEM results also provided via NNUF

## Slide 7: Results I
SWIR spectra for all Split SIMFuel pellets by dopant group
False colour image of the Split SIMFuel pellet surfaces arrangement by dopant group

## Slide 8: Results II
Mean SWIR spectra for Split SIMFuel pellets by dopant group
Index of the two main features for Split SIMFuel pellets by dopant group

## Slide 9: Overall Dataset
Dataset of 3 pellet groups
Response across the groups is clear, consistent, and repeatable
SIMFuel, pure and doped UO2
AGR fuel pellets, pure UO2
NNUF
Split SIMFuel, pure and doped UO2
Split SIMFuel indexed comparison

## Slide 10: Conclusions, Ongoing work, and Thanks
Dataset of 3 pellet groups, response is clear, consistent, and repeatable
Appears that the presence of Lanthanide causes significant spectral response change
Short communication in preparation
Full analysis of Raman and SEM is ongoing to understand spectral features (peaks and absorptions bands
THANKS to …